Plastics 001 	                                             	    Name_______________________

______________

Exam #3                               		           76                                        Date____________________

- Why can you get better surface finish with Injection Molding compared to Extrusion or Extrusion Blow Molding? (2 pts)

___________________________________________________________________________________________________

- How can you tell if the plastic part that you have is made with Injection Molding? (2 pts)

___________________________________________________________________________________

- What causes the screw in an Injection Molding machine to be pushed towards the back of the injection unit during the plastification stage? (2 pts)

____________________________________________________________________________________________________

- What completes/finishes the packing stage in Injection Molding? (2 pts)

____________________________________________________________________________________________________

- Which Injection Molding process variation puts a second material inside the part between the first material? (2 pts)

____________________________________________________________________________________________________

- Why would you pick Injection Molding as a process to make a part over any other plastics process? (2 pts)

____________________________________________________________________________________________________

- Why can Injection Molded parts have higher tolerances compared to other plastics processes?  (2 pts)

_____________________________________________________________________________________________________

- Name 2 advantages of Injection Molding: (2 pt each)

  - ___________________________________________________________

  - ___________________________________________________________

- Name 2 disadvantages of Injection Molding: (2 pt each)

  - ___________________________________________________________

  - ___________________________________________________________

- How can you distinguish a Profile Extrusion part from and Injection Molded part? (2 pts)

_____________________________________________________________________________________________________

- Why would you need to cool the barrel of an Extruder while it is making a part? (2 pts)

_____________________________________________________________________________________________________

- What does a sizing die do in Profile Extrusion? (2 pts)

_____________________________________________________________________________________________________

- What makes the polymer extrudate move through the cooling tank? (2 pts)

_____________________________________________________________________________________________________

- What type of die is used in Blown Film Extrusion? (2 pts)

_____________________________________________________________________________________________________

- What polymer property is needed so the extrudate in Profile Extrusion does not break, before it cools, as it moves through the cooling tank? (2 pts)

_____________________________________________________________________________________________________

- What is die swell in Profile Extrusion? (2 pts)

_____________________________________________________________________________________________________

- Name 2 advantages of Profile Extrusion: (2 pt each)

  - ___________________________________________________________

  - ___________________________________________________ ________

- Name 2 disadvantages of Profile Extrusion: (2 pt each)

  - ___________________________________________________________

  - ___________________________________________________________

- Which Blow Molding process can make larger parts? (2 pts)

_____________________________________________________________________________________________________

- What two methods can be used to get air inside of the hollow extruded tube in Extrusion Blow Molding? (2 pts)

_____________________________________________________________________________________________________

- What is the hollow extruded tube called in Extrusion Blow Molding? (2 pts)

_____________________________________________________________________________________________________

- In Intermittent Extrusion Blow Molding, where is the polymer stored while the mold is closed? (2 pts)

_____________________________________________________________________________________________________

- What causes sag in Extrusion Blow Molding? (2 pts)

_____________________________________________________________________________________________________

- Name 2 advantages of Extrusion Blow Molding: (2 pt each)

  - ___________________________________________________________

  - ___________________________________________________________

- Name 2 disadvantages of Extrusion Blow Molding: (2 pt each)

  - ___________________________________________________________

  - ___________________________________________________________

- What is the maximum sized bottle that can be made in Injection Blow Molding? (2 pts)

_____________________________________________________________________________________________________

- What is the Injection Molded tube called in Injection Blow Molding? (2 pts)

_____________________________________________________________________________________________________

- What are two ways to condition an Injection Molded tube in Injection Blow Molding? (2 pts)

_____________________________________________________________________________________________________

- Name 2 advantages of Injection Blow Molding: (2 pt each)

  - ___________________________________________________________

  - __________________________________________________ ________

- Name 2 disadvantages of Injection Blow Molding: (2 pt each)

  - ___________________________________________________________

  - __________________________________________ ________________