Plastics 001	                                             	    Name__Master_______________

______________

Exam #3                               		           76                                        Date____________________

- Why can you get better surface finish with Injection Molding compared to Extrusion or Extrusion Blow Molding? (2 pts)

___Because you are filling and packing under high pressure.  This helps pick up more detail in the mold________________

- How can you tell if the plastic part that you have is made with Injection Molding? (2 pts)

__If the part has good surface finish and interior part detail, then it most likely is Injection Molding_________________

- What causes the screw in an Injection Molding machine to be pushed towards the back of the injection unit during the plastification stage? (2 pts)

___The pressure built up as the polymer is pumped in front to f the screw________________________________________

- What completes/finishes the packing stage in Injection Molding? (2 pts)

___Gate freeze________________________________________________________________________________________

- Which Injection Molding process variation puts a second material inside the part between the first material? (2 pts)

___Sandwich Molding___________________________________________________________________________________

- Why would you pick Injection Molding as a process to make a part over any other plastics process? (2 pts)

___If you need high tolerances, good surface detail, or interior features___________________________________________

- Why can Injection Molded parts have higher tolerances compared to other plastics processes?  (2 pts)

___Because the packing phase can compensate for polymer shrinkage.  This phase is not present in the other processes____

- Name 2 advantages of Injection Molding: (2 pt each)

  - _ High Production Rates, High Tolerances, Hot Runners – Low Scrap Rate,_______

  - _ Minimal Labor, Complex Shapes, and Excellent Surface Finish _______________

- Name 2 disadvantages of Injection Molding: (2 pt each)

  - _ High Tooling Cost, Part Details not Easy to Construct, Warpage after Molding,___

  - _ Long Mold Building Time, and Hard to Predict Shrinkage ___________________

- How can you distinguish a Profile Extrusion part from and Injection Molded part? (2 pts)

___Extrusion parts have a 2D cross-section and a constant third dimension.  They also can have drag marks running along the third dimension________________________________________________________________________________________

- Why would you need to cool the barrel of an Extruder while it is making a part? (2 pts)

___Because of frictional heating in the barrel________________________________________________________________

- What does a sizing die do in Profile Extrusion? (2 pts)

___It helps to keep the extrudate in shape__________________________________________________________________

- What makes the polymer extrudate move through the cooling tank? (2 pts)

___The puller__________________________________________________________________________________________

- What type of die is used in Blown Film Extrusion? (2 pts)

___Tubular____________________________________________________________________________________________

- What polymer property is needed so the extrudate in Profile Extrusion does not break, before it cools, as it moves through the cooling tank? (2 pts)

___Melt strength/High viscosity____________________________________________________________________________

- What is die swell in Profile Extrusion? (2 pts)

___The polymer chains are quickly oriented as they enter the die.  When they exit the die, they want to go back to their original orientation______________________________________________________________________________________________

- Name 2 advantages of Profile Extrusion: (2 pt each)

  - _High production rates, low tooling costs,_________________________________

  - _Lowest cost conversion process for plastics_______________________________

- Name 2 disadvantages of Profile Extrusion: (2 pt each)

  - _Secondary operations for 3rd dimension, tolerance issues,___________________

  - _Long die debug time, and surface defects_________________________________

- Which Blow Molding process can make larger parts? (2 pts)

___Extrusion Blow Molding______________________________________________________________________________

- What two methods can be used to get air inside of the hollow extruded tube in Extrusion Blow Molding? (2 pts)

___Blow Pins and blow needles___________________________________________________________________________

- What is the hollow extruded tube called in Extrusion Blow Molding? (2 pts)

___Parison____________________________________________________________________________________________

- In Intermittent Extrusion Blow Molding, where is the polymer stored while the mold is closed? (2 pts)

___In the accumulator___________________________________________________________________________________

- What causes sag in Extrusion Blow Molding? (2 pts)

___Gravity____________________________________________________________________________________________

- Name 2 advantages of Extrusion Blow Molding: (2 pt each)

  - _Inexpensive molds, complex geometry, combine features,____________

  - _Foam filled_________________________________________ ________

- Name 2 disadvantages of Extrusion Blow Molding: (2 pt each)

  - _Filling problems, cooling on one side, warpage, flash, weld failure,___

  - _Secondary operations, uneven wall thickness, and surface finish_____

- What is the maximum sized bottle that can be made in Injection Blow Molding? (2 pts)

___5 gallons___________________________________________________________________________________________

- What is the Injection Molded tube called in Injection Blow Molding? (2 pts)

___Preform____________________________________________________________________________________________

- What are two ways to condition an Injection Molded tube in Injection Blow Molding? (2 pts)

___Heating and cooling__________________________________________________________________________________

- Name 2 advantages of Injection Blow Molding: (2 pt each)

  - _Bi-axial orientation, no scrap, good surface finish, _________________

  - _and Tighter tolerance________________________________________

- Name 2 disadvantages of Injection Blow Molding: (2 pt each)

  - _Small size, higher tooling costs, ________________________________

  - _and offset neck bottles cannot be made__________________________