Plastics 001	                                               	    Name______________

______________

Quiz #5                                                              53                                                           Date___________

- List the four commodity polymers, list 4 advantages and 2 disadvantages of each. (32 pts)

- HDPE

AD 1    Excellent Chemical Resistance

AD 2    Ductile

AD 3    Easily Recyclable

AD 4    Inexpensive; Easily Processed

Dis 1    Extremely Flammable

Dis 2    Difficult to Decorate + Assemble; Low Dimensional Stability

- PP

AD 1    Easily Recyclable

AD 2    Chemically Resistant

AD 3    Easily Processed

AD 4    Inexpensive; Living hinge

Dis 1    Low Dimensional Stability

Dis 2    Poor Weatherability; Difficult to Decorate + Assemble

- PVC

AD 1    Good Electrical Properties

AD 2    Good Chemical Resistance

AD 3    Good Weatherability

AD 4    Variety of Hardnesses; Dimensionally stable

Dis 1    Difficult to Recycle (HCl)

Dis 2    Not Thermally Stable; Phthalates or Plasticizers

- GPPS

AD 1    Good Optical Properties

AD 2    Dimensionally Stable

AD 3    Easy to Decorate + Assemble

AD 4    Good Insulator; Easily Processed; Easily Recyclable

Dis 1    Flammable

Dis 2    Poor Chemical Resistance; Brittle

- List 2 applications for each of the commodity polymers that were listed in the reading you were supposed to do for the lesson. (16 pts)

  - HDPE

1]    Just about anything that sounds reasonable

2]    __________________________________

  - PP

1]    Just about anything that sounds reasonable

2]    __________________________________

  - PVC

1]    Just about anything that sounds reasonable

2]    __________________________________

  - GPPS

1]    Just about anything that sounds reasonable

2]    __________________________________

- What is the difference between when a commodity plastic and an engineering plastic are chosen for a specific application? Usually when a plastic is being decided on for a specific part, you are either looking at a commodity or an engineering resin what causes you to make that choice between which one to look for at the onset of the material search? (5 pts)

Based on mechanical properties

_____________________________________________________________________________

_____________________________________________________________________________

_____________________________________________________________________________

Ex. (1 each)

What are CD’s made of?  PC

What are computer housings made of? ABS

What are tail lights on cars made of? PMMA or PC

What are the clasps on your backpack made of? POM

What are zip ties made of? Nylon or PA